VIRIDIAN v lam Soft white or translucent

Glass shall be Viridian VLam,  	 * thick, incorporating 			PVB interlayer.

* Glass Thicknesses available are –6.38mm 8.38mm, 10.38mm, 12.38mm

PVB Interlayer Options include: Soft White or White Translucent.

The glass shall comply with the following performance criteria:

| Visible Light Transmission % | U Value | Shading Co-efficient (SC) | Solar Heat Gain Coefficient (SHGC) |
| --- | --- | --- | --- |

Solar control glass may be subject to thermal stress and should therefore be thermally assessed prior to installation.

All glass is to be selected and installed in accordance but not exclusively with the following Australian and/or New Zealand Standards

- AS 1288 Glass in Buildings Selection and Installation

- AS 1170 Minimum Wind Loads on Structures

- AS/NZ 2208 Safety Glazing Materials in Buildings

- AS/NZ 4666 Insulating Glass Units

- AS/NZ 4667 Quality Requirements for cut-to-size and Processed Glass